## Slide 1: Development of a MoS₂/PEDOT:PSS Functionalized Electrode for Trace-Level Detection of Toxic Hg2+

## Slide 2
What is MoS2 & PEDOT:PSS ?
MoS₂ (molybdenum disulfide) is a two-dimensional transition metal dichalcogenide composed of layered S–Mo–S sheets, exhibiting semiconducting behavior, high surface area, and excellent electrocatalytic and electronic properties at the nanoscale.
Due to its large active surface, good charge carrier mobility, and strong interaction with analytes, MoS₂ is widely used in sensing, energy storage, and catalytic applications.
PEDOT:PSS is a conductive polymer composite consisting of poly(3,4-ethylenedioxythiophene) (PEDOT) as the conducting component and poly(styrene sulfonate) (PSS) as the charge-balancing and film-forming polyelectrolyte.
It exhibits high electrical conductivity, flexibility, optical transparency, and good film-forming ability, making it suitable for electrodes, biosensors, and flexible electronic devices.
The combination of MoS₂ and PEDOT:PSS provides synergistic advantages, including enhanced charge transfer, increased active surface area, and improved stability, which are highly beneficial for electrochemical sensing platforms.

## Slide 3
Hydrothermal Method and polymerization
The hydrothermal method is a solution-based synthesis technique carried out in a sealed autoclave at elevated temperature and pressure, enabling controlled crystal growth of nanomaterials from aqueous precursors.
This method promotes high crystallinity, controlled morphology, and uniform particle size, making it widely used for preparing metal oxides, sulfides, and other functional nanostructures.
Chemical polymerization is a synthesis process in which monomer units are chemically oxidized to form long polymer chains, commonly used for preparing conducting polymers such as PEDOT.
In this method, an oxidizing agent initiates polymer chain formation, while dopants or polyelectrolytes (like PSS) improve conductivity, stability, and processability of the resulting polymer.
Both hydrothermal synthesis and chemical polymerization are important for developing advanced nanocomposites, as they allow control over structure, composition, and functional properties required for sensing and electronic applications.

## Slide 4
Synthesis of MoS2 nanosheets

## Slide 5
Solution A
EDOT
Addition of solution B to solution A
Solution B
FeCl3
FeCl3
Kept in constant stirring @90°C for 0.5h
Solution A
Solution A+B
Solution transferred to vacuum flask
Freeze dried
and stored
After grinding
PEDOT PSS Powder
Synthesis of PEDOT-PSS

## Slide 6: FE-SEM Analysis of PEDOT:PSS

## Slide 8: FE-SEM Analysis of MoS2

## Slide 10: FE-SEM Analysis of PEDOT:PSS/MoS2

## Slide 12: FTIR SPECTRUM PEDOT:PSS/MoS2

## Slide 13
PEDOT-PSS/MoS2
MoS2
PEDOT-PSS

## Slide 14
FTIR Spectral Analysis
The FTIR spectra display characteristic peaks of PEDOT:PSS and MoS₂, confirming the presence of both components in the composite material.
The PEDOT:PSS/MoS₂ spectrum shows combined vibrational features with slight shifts and intensity changes, indicating successful interaction and formation of the hybrid composite structure.
Peaks related to the thiophene ring vibrations and sulfonate groups of PEDOT:PSS are retained, demonstrating that the polymer backbone remains chemically stable after composite formation.
Characteristic Mo–S vibrational modes in the low wavenumber region confirm the structural integrity of MoS₂ within the composite.
The absence of new impurity peaks suggests good compatibility between PEDOT:PSS and MoS₂, supporting the formation of a well-integrated nanocomposite suitable for electronic and sensing applications.

## Slide 15: X-Ray Diffractogram PEDOT:PSS/MoS2

## Slide 16
PEDOT-PSS/MoS2

## Slide 17
XRD Diffractogram Analysis
The XRD pattern of the PEDOT:PSS/MoS₂ composite shows characteristic diffraction peaks corresponding to crystalline MoS₂, confirming its structural retention within the hybrid material.
A broad background feature associated with PEDOT:PSS indicates the amorphous nature of the conducting polymer matrix.
The coexistence of sharp MoS₂ peaks and the broad polymer halo demonstrates successful incorporation of MoS₂ into the PEDOT:PSS framework without phase decomposition.
No additional impurity peaks are observed, suggesting good phase purity and compatibility between the inorganic MoS₂ and organic polymer components.
The composite structure supports enhanced interfacial interaction, which is beneficial for charge transport and electrochemical sensing performance.

## Slide 18: Electrochemical sensing of Mercury (Hg2+)

## Slide 19
Method of standard addition
5µM
55µM
SWASV Voltammograms for the sensitive detection of Hg2+ ions using PEDOT:PSS/MoS2 modified Glassy carbon electrode from 5µM to 55µM
Hg2+

## Slide 20
Linear range and Lod Calculation
𝐿𝑂𝐷 = 3.3×Standard deviation/slope
The Calibration plot between the oxidation peak currents vs. the concentration of Mercury (Hg2+) (n = 3).

## Slide 21
Interference effect of Other heavy metals
SWASV voltammograms illustrating the mutual interference analysis of heavy metal ions, demonstrating the sensor's capability to maintain distinct and well-defined anodic peaks with minimal cross-interference, even under varying analyte concentrations.
Hg2+
Cu2+
Pb2+
Cd2+

## Slide 22
0 µM- 100µM
0 µM- 100µM
0 µM- 100µM
50µM

## Slide 23
Hg2+
Cu2+
Pb2+
Cd2+

## Slide 24
50 µM
50 µM
50 µM
50- 200 µm

## Slide 25: THANK YOU